Table 6. Los Angeles Abrasion Test Results
	Aggregate Type
	Initial Weight (g)
	Final Weight (g)
	Weight Loss (g)
	Percentage Loss (%)
	ASTM C131/C535 Limit (Max 40-50%)

	Fresh Aggregate
	5000
	4350
	650
	13.00%
	Complies

	Recycled Aggregate
	5000
	3900
	1100
	22.00%
	Complies



