Table 6. Los Angeles Abrasion Test Results

| Aggregate Type | Initial Weight (g) | Final Weight (g) | Weight Loss (g) | Percentage Loss (%) | ASTM C131/C535 Limit (Max 40-50%) |
| --- | --- | --- | --- | --- | --- |
| Fresh Aggregate | 5000 | 4350 | 650 | 13.00% | Complies |
| Recycled Aggregate | 5000 | 3900 | 1100 | 22.00% | Complies |