Table 7. Aggregate Crushing Value (ACV) Test Results (As per IS: 2386 Part-4)

| Aggregate Type | Weight of Sample (g) | Weight of Crushed Material Passing 2.36 mm Sieve (g) | Aggregate Crushing Value (ACV) (%) | IS Standard Limit (Max 30-45% for Sub-base & Base Courses) |
| --- | --- | --- | --- | --- |
| Fresh Aggregate | 4000 | 720 | 18.00% | Complies (Good for all pavement layers) |
| Recycled Aggregate | 4000 | 1080 | 27.00% | Complies (Suitable for sub-base/base layers) |