Table 7. Aggregate Crushing Value (ACV) Test Results (As per IS: 2386 Part-4)
	Aggregate Type
	Weight of Sample (g)
	Weight of Crushed Material Passing 2.36 mm Sieve (g)
	Aggregate Crushing Value (ACV) (%)
	IS Standard Limit (Max 30-45% for Sub-base & Base Courses)

	Fresh Aggregate
	4000
	720
	18.00%
	Complies (Good for all pavement layers)

	Recycled Aggregate
	4000
	1080
	27.00%
	Complies (Suitable for sub-base/base layers)



