INFRARED (IR) SPECTROSCOPY REPORT

Objective:- To confirm the presence of characteristic functional groups (aldehyde C=O, polyene C=C, nitrile C≡N) in the synthesized polyene chromophore aldehyde using FT-IR spectroscopy.

1. Experimental Procedure

Sample Preparation

Materials:

- Synthesized polyene aldehyde (1–2 mg)

- Potassium bromide (KBr, 100 mg, IR-grade)

- Hydraulic pellet press

Steps:

- Grinding: Mix 1–2 mg of sample with 100 mg dry KBr in an agate mortar.

- Pellet Formation: Press the mixture into a transparent pellet using a hydraulic press (10–15 tons for 1–2 min).

- Loading: Place the pellet in the FT-IR sample holder.

Instrumentation

- Spectrometer: Shimadzu IRTracer-100 FT-IR

- Scan Range: 4000–400 cm⁻¹

- Resolution: 4 cm⁻¹

- Scans per Sample: 32 (to improve signal-to-noise ratio)

- Background Correction: Pure KBr pellet used as reference.

2. Data Acquisition & Processing

- Background Scan: Run a blank KBr pellet to subtract atmospheric CO₂/H₂O interference.

- Sample Scan: Place the sample pellet and acquire the spectrum.

- Baseline Correction: Apply automatic baseline correction to remove scattering effects.

- Peak Picking: Identify key absorption bands using Shimadzu LabSolutions IR software.

3. IR Spectrum & Interpretation

Observed Peaks & Assignments

| Wavenumber (cm⁻¹) | Intensity | Assignment | Vibration Mode |
| --- | --- | --- | --- |
| 3060 | Weak | =C–H (polyene/aromatic) | Stretch |
| 2920 | Medium | –CH₃/–CH₂– | Asymmetric stretch |
| 2850 | Medium | –CH₃/–CH₂– | Symmetric stretch |
| 2720 | Weak | Aldehyde C–H | Fermi resonance (overtone of C=O) |
| 1695 | Strong | Aldehyde C=O | Stretch (conjugated) |
| 1620–1600 | Medium | C=C (polyene) | Stretch |
| 1585 | Medium | C=C (aromatic) | Ring stretch |
| 1500 | Medium | C=C (aromatic) | Ring stretch |
| 2240 | Weak | C≡N (nitrile) | Stretch |
| 1450 | Medium | –CH₂– | Scissoring |
| 1375 | Medium | –CH₃ | Symmetric bend |
| 1100–1000 | Variable | C–O/C–N | Stretch |

Key Observations

- Aldehyde Confirmation:

- Strong peak at 1695 cm⁻¹ (C=O stretch, shifted lower due to conjugation).

- Weak Fermi resonance band at 2720 cm⁻¹ (characteristic of aldehydes).

- Polyene System:- C=C stretches at 1620–1600 cm⁻¹ (conjugated diene/triene). Aromatic C=C at 1585, 1500 cm⁻¹.

- Nitrile Retention:- Weak but sharp peak at 2240 cm⁻¹ (C≡N stretch from cyanoacetamide precursor).

- No Impurities:-Absence of O–H (3300 cm⁻¹) or N–H (3400 cm⁻¹) peaks confirms no residual solvent/starting material.

4. Comparison with Theoretical Values

| Functional Group | Expected Range (cm⁻¹) | Observed (cm⁻¹) | Deviation |
| --- | --- | --- | --- |
| Aldehyde C=O | 1725–1705 (non-conj.) | 1695 | ↓ 30 cm⁻¹ (due to conjugation) |
| Polyene C=C | 1650–1600 | 1620–1600 | Matched |
| Aromatic C=C | 1600–1450 | 1585, 1500 | Matched |
| C≡N | 2260–2210 | 2240 | Matched |

Note: The lower C=O stretch (1695 cm⁻¹) is expected due to conjugation with the polyene system, which delocalizes the π-electrons and reduces bond order.

5. Troubleshooting & Validation

- Broad C=O peak? May indicate hydrogen bonding (use dry solvent/KBr).

- Missing C≡N peak? Check if nitrile was hydrolyzed during synthesis (confirm with ¹H-NMR).

- Water interference? Ensure KBr is anhydrous (dry at 110°C for 2 hrs).

6. Conclusion

- Successful synthesis confirmed by:

- Aldehyde C=O (1695 cm⁻¹) and polyene C=C (1620–1600 cm⁻¹).

- Retention of nitrile group (2240 cm⁻¹).

- No detectable impurities (e.g., –OH, –NH₂).